## Slide 1: Sapphire for the LCGT project
Eiichi Hirose
ICRR, University of Tokyo
Kyohei Watanabe, Norikatsu Mio
PSC, University of Tokyo

## Slide 2: LCGT project
Laser
PRM
BS
SRM
ITMX
ITMY
ETMX
ETMY
38cm dia.
10cm dia.
Sapphire
The others are all silica
@ low temperature, sapphire has
high mechanical Q (low loss)
large heat conductivity
Requirements to sapphire
25cm dia. x 15 thickness (30 kg)
absorption < 20ppm/cm
orientation < 0.04 deg
Underground
Low seismic noise
Cryogenic mirrors and suspensions
Reduction of thermal noise
Tokyo
Gifu
Project got started last September and now under construction

## Slide 3: A few methods to measure optical absorption
Laser calorimeter
Changes index of refraction
Changes optical length => interferometer
Changes direction of laser beam => Photo-thermal deflection method
Causes thermal expansion
Causes a sound wave => Photo-acoustic detection
Basic idea is that small optical absorption changes temperature

## Slide 4: Photo-thermal deflection method
C-axis 100 mm dia. x 60 mm thickness
Z=10mm, 54,2 ppm/cm
Z=20mm, 46.1 ppm/cm
Z=30mm, 47.3 ppm/cm
Z=40mm, 45.5 ppm/cm
Z=50mm, 53.4 ppm/cm
Z=30mm (2005)

## Slide 5: Interferometric method
Lock-in Amplifier
PZT
PD
Mirror1
Laser
λ：1064nm
Power：10W
120Hz
Chopper
BS(R:98%)
BPF
PZT driver
LPF
Filter
15kHz
Chopped light is incident on a sample.
Signal is lock-in detected.
Drak fringe
Sample
Mirror2
BS
Sample
light power
absorbed
temperature
change
Refraction Index,
sample’s length
change
Optical path
Length change

## Slide 6: Result for BK7
Heat Equation
energy source from
laser light
FEA (Finite Element Analysis)
Is used to calculate absorption
80pm/W (L = 10mm)
284pm/W (L = 40mm)
20 mm dia.
-2pm/W w/o sample
radial
axial
Temperature change Max: 0.01 degC
0.6 mm
0.6 mm
BK7
Laser dia. = 0.1 mm
The more input power , the longer
Optical absorption
10mm: 2230 ppm/cm
40mm: 2300 ppm/cm
Standard glass ,
optical absorption (10-3-10-4 /cm)
L
✓

## Slide 7: Calibration
Comparison with another method
A thermistor is attached on a lateral surface of the BK7 sample in order to measure the temperature change of the sample.
The difference between the gradient of the temperature change is almost independent of the boundary condition.
The experimental data and the numerical simulation are consistent.
On
Off
On
Off
Big difference from the other method
Optical absorption
1600 ppm/cm
✓

## Slide 8: Sapphire sample
  C-axis rod (10mm dia., 40mm length)

## Slide 9: Preliminary result
AA149 | 48 | 47 |  | 
AC150 | 229 | 138 | 682 | 687
P401 | 34 | 32 | 65 | 67
absorption [ppm/cm]
10 Samples
AC150 shows quite high absorption. why ?
P401 contains lower pair and high absorption pair. What is the difference?

## Slide 10: Conclusion
LCGT project started last year and the detector is under construction
We need sapphire that meets the requirement
Measured absorption and the result shows some variation from sample to sample

## Slide 11: AA149
1:7.3pm/W→48ppm/cm
2:7.2pm/W→47ppm/cm

## Slide 12: AC150
1:35.2pm/W→229ppm/cm
2:21.2pm/W→138ppm/cm
3:104.7pm/W→682ppm/cm
4:103.9pm/W→677ppm/cm

## Slide 13: P401
5.2pm/W
34ppm/cm
5.0pm/W
32ppm/cm
9.9pm/W
65ppm/cm
10.3pm/W
67ppm/cm