## Slide 1
Items
  ** two beam tubes of 3-km long and 800 mm in diameter
  ** optical baffles distributed at every 12 meter in the beam tubes
  ** beam monitor target inserted in the beam tubes
  ** chambers for the mirrors with suspension and vibration-isolation devices
  ** vacuum pumping system
  ** overall layout
Interface
  all of the subsystem groups; entire systems is in an un-separated vacuum.
  ** choice of materials for components used in cryostat, optical devices,
    vibration-isolation devices, . . .
  ** interferometer layout and operation sequence
cf. vacuum system philosophy in accelerator
  ** beam dynamics and vacuum system have to be designed simultaneously.
  ** choice of materials having low outgassing is most important.
  ** mechanical and electric design of every component has to be simple.
  ** materials properties have to be examined and measured before choosing.
  (KEK Internal 07-17)
1. Overview
120418 VAC (YS)
KAGRA Vacuum System

## Slide 2
  ** We predict the noise dx due to the residual gas (water) molecules;
  for dx = 1×10-21 m/√Hz@100 Hz (safety margin of 10),
  the pressure in the beam tubes is to be kept at 2×10-7 Pa.
      (h=3×10-24 /(Hz)1/2 @100Hz corresponds to dx=1×10-20 m/(Hz)1/2)
<<scattering effect due to residual gas>>
  ** For long-term and stable operation of the interferometer, the vacuum system is to be designed so as to minimize the maintenance work, and so as to shorten the pump-down time. A long lifetime of the vacuum component and low outgassing is required.
<<minimize the maintenance work>>
Ti cathode
Penning cell
Required Pressure：
in the order of 10-7 Pa, or lower
2. Target specifications
120418 VAC (YS)
KAGRA Vacuum System

## Slide 3
KAGRA Vacuum System
ETMYA
ITMY
ETMXA
ITMX
IP
TMP
FL P
BS
PRM
PR3
PR2
SRM
SR3
SR2
PD
MCF
MC
3000 m
IAOX
EAOX
MMT
BRTY
BRTX
Layout:
less changes “i” to “b”
IAOY
EAOY
ETM: end test mass
ITM: input test mass
BS: beam splitter
IAO/EAO: auxiliary optics of input/end
MC: mode cleaner
PRM: power recycling mirror
SRM: signal recycling mirror
PD: photo detector
BRT: beam reducing telescope.
120418 VAC (YS)
2. Target specifications
Type A double chamber (2.4 and 1.5 m in dia.)
//GASF + I-Pendulum + cryogenic//
Type C chamber
(1.5 m in dia./ 2 m for MC)
//stack + D-Pendulum//
two beam tubes of 3-km long and 800 mm in dia.
//optical baffles at every 12 meter
//pumping unit at every 100 meter
Type B chamber
(1.5 m in dia./2 m for BS)
//GASF + I-Pendulum//

## Slide 4
x
y
Yopt
horizontal plane at center room
horizontal plane at X end
Y arm
optical plane of interferometer
X arm
BS
ETMX
ETMY
X arm
Y arm
ITMX
ITMY
Xopt
Yopt
O
Xopt
O (BS)
iLCGT
1/300
horizontal plane at Y end
120418 VAC (YS)
KAGRA Vacuum System
Layout:
horizontal floors for installing chambers
2. Target specifications

## Slide 5
Beam tube (478 of 12-m long and 0.8 m in diameter); 320 tubes completed, so far.
3. Final design and quality assurance; (1) Beam tube
120418 VAC (YS)
KAGRA Vacuum System
“surface passivation by electro-polish followed by baking”
      outgassing rate; 10-8 Pa m3 m-2 s-1, or lower
      surface roughness; Rmax 3 mm, Ra 0.5 mm
“mirror finish by Electro-Chemical Buffing (tubes in the mid 800-m region)”
      surface roughness; Rmax 0.2 mm, Ra 0.03 mm
“flange connection with metal O-ring (silver plated)”; erosion proof by humidity test
Electro-polished tube of 12 m long
Electro-chemical buffed tube of 12 m long

## Slide 6
Manufacturing process of a beam tube (12-m long and 0.8 m in diameter
120418 VAC (YS)
KAGRA Vacuum System
* hot roll → austenitic process (Annealing & Pickling) → surface grinding
11.2-m long
8-mm thick
2.5-m wide
SS 304L
Surface finish condition
  grinding: Grit # 150, wet
  Ry ~ 8 mm
Sumikin & Nippon Steel Stainless Steel Pipe Co., Noda
3. Final design and quality assurance; (1) Beam tube

## Slide 7
Manufacturing process of a beam tube (12-m long and 0.8 m in diameter
120418 VAC (YS)
KAGRA Vacuum System
* press forming → one-seam weld (plasma welding without filler)
11.2-m long
0.8 m in diameter
geometrical tolerance
  straightness: 0.1%/L
  circularity: 1%/D
  perpendicularity: 0.2%/D
Sumikin & Nippon Steel Stainless Steel Pipe Co., Noda
3. Final design and quality assurance; (1) Beam tube

## Slide 8
Manufacturing process of a beam tube (12-m long and 0.8 m in diameter
120418 VAC (YS)
KAGRA Vacuum System
* flanges
flange
  SS F 304; rotary forging
  thickness; 30 mm
  welding neck; 120 mm long
  flatness: 0.1 mm
  SS F 304; rotary forging
Shimoda Iron Works Co., Aioi /Yamashita Tanzosho Co., Katano
3. Final design and quality assurance; (1) Beam tube

## Slide 9
Manufacturing process of a beam tube (12-m long and 0.8 m in diameter
120418 VAC (YS)
KAGRA Vacuum System
Austenitic process and machining: Shimoda Iron Works Co., Aioi
* flanges
flange
  SS F 304; rotary forging
  thickness; 30 mm
  welding neck; 120 mm long
  flatness: 0.1 mm
3. Final design and quality assurance; (1) Beam tube

## Slide 10
Manufacturing process of a beam tube (12-m long and 0.8 m in diameter
120418 VAC (YS)
KAGRA Vacuum System
* bellows
bellows
  SS316L; hydroformed
  stiffness; 100 N/mm or less
  finish: chemical polishing
Nippon Shinshukukan Co., Hosono
3. Final design and quality assurance; (1) Beam tube

## Slide 11
Manufacturing process of a beam tube (12-m long and 0.8 m in diameter
120418 VAC (YS)
KAGRA Vacuum System
3. Final design and quality assurance; (1) Beam tube
* weld flanges and bellows
MIRAPRO Co., Noda

## Slide 12
Manufacturing process of a beam tube (12-m long and 0.8 m in diameter
120418 VAC (YS)
KAGRA Vacuum System
3. Final design and quality assurance; (1) Beam tube
* electro polishing and rinsing
electro polishing
  current density; 20 A/dm2
  removal; 30-40 mm
  Ry ~ 2.5 mm
rinsing
  pure water; 15 MW
Electro polishing;
San-ai Plant Co., Kisarazu / Marui Galvanizing Co., Kashiwa
#150 grinding
（15 μm removal）
（25 μm removal）
35 μm removal）

## Slide 13
Manufacturing process of a beam tube (12-m long and 0.8 m in diameter
120418 VAC (YS)
KAGRA Vacuum System
3. Final design and quality assurance; (1) Beam tube
* vacuum baking
  → dry air venting (-40°C dew point)
  → seal (EPDM gasket)
MIRAPRO Co. Noda/MESCO, Kamioka
furnace（200℃，〜3days）

## Slide 14
Chart: pumping time [hours]
Cu (PR-EF lining, 2nd pump.): ID 560 X L 3000 | 5.2e-08
120418 VAC (YS)
KAGRA Vacuum System
1 10 100 1000
Measured outgassing rate of a beam tube
3. Final design and quality assurance; (1) Beam tube

## Slide 15
120418 VAC (YS)
KAGRA Vacuum System
3. Final design and quality assurance; (1) Beam tube
Storage beam tube (one year, or more)
A tunnel of Kamioka Mining Railway (not in service)

## Slide 16
N=(h/d)/(L/R)
** estimated scattered light noise at Kamioka
  dx = 3×10-21 m/√Hz@30Hz (tube vibration amplitude=1×10-11 m/√Hz assumed )
** For more margin, baffles at “every 12 meters”. dx = 5×10-22 m/√Hz
** For randomizing phase of edge-scattered light, baffles with “saw-tooth edge”.
Every12-m along the arm, 40-mm in height, 50-degree tilted
3. Final design and quality assurance; (2) Optical baffles in beam tubes
120418 VAC (YS)
KAGRA Vacuum System

## Slide 17
Coating of diamond-like-carbon (DLC) film of 1 mm thick
3. Final design and quality assurance; (2) Optical baffles in beam tubes
120418 VAC (YS)
KAGRA Vacuum System
Black finishing | UB-NiP | Phosblack-II | DLC | Raydent
Absorption coeff.（%） | 99.89 | 85 | 65 | 83
Tomaru et. al, J. Vac. Soc. Jpn, 48, 2005
cross = p, open circle = s:
Takahashi et. al, Vacuum 73, 2004
DLC coated
Mirror polished SS
outgassing rate = 4×10-9 Pa m3 m-2 s-1
absorption coefficient = 65% @ 0 deg
reflectivity = 0.1 - 0.2 @ 45-60 deg

## Slide 18
** Although the aluminum-coated thin PET (polyethylene terephtalate) film is suitable material for thermal shield, the outgassing rate is higher than those of metal surfaces.
Outgassing measurement of Al-coated PET laminations
3. Final design and quality assurance; (3) PET laminations for thermal shield
120418 VAC (YS)
KAGRA Vacuum System
CLIO cryostat

## Slide 19
** Although the aluminum-coated thin PET (polyethylene terephtalate) film is suitable material for thermal shield, the outgassing rate is higher than those of metal surfaces.
** Outgassing rate of a PET film of 12 micrometer thick is measured.
The rate decreases to 10-6 Pa m3 s-1 m-2 for about 10h, then reaching to the order of 10-8 Pa m3 s-1 m-2 for 200h.
** Water molecules absorbed in film is possibly diffused to the surface
and desorbed with a long period of 100 hours.
Outgassing measurement of Al-coated PET laminations
3. Final design and quality assurance; (3) PET laminations for thermal shield
Chart: pumpimg time [hours]
120418 VAC (YS)
KAGRA Vacuum System

## Slide 20
Pumping system (dry-pump and ion-pump)
3. Final design and quality assurance; (4) Vacuum system operation
120418 VAC (YS)
KAGRA Vacuum System
** pumping unit is distributed “every 100 meters” along tubes.
** pumping speed of the unit (100 m)
  600 m3/h >> dry-pump
  2000 L/s >> TMP
  500 L/min >> TMP foreline pump
  1000 L/s >> IP
ETMX
ITMX
IP
TMP
FL P
3000 m
DRY P
“expected pump-down scheme (a 3-km arm)”
  to 1 Pa >> few days by dry-pump
  to 10-6 Pa >> 50 hours by TMP
  to 10-7 Pa >> 500 hours by ion pump
(based on the ougassing rate in test tubes)
“maintenance without breaking arm-vacuum”
  ion pump life, B-A gauge failure,
  feed-through erosion, . . .
  durability for humidity is being examined (50°C-98%) for vacuum components.
“fail-safe by closing gate valves (large dia,)”
    electric-power shut down
    anomalous pressure rise

## Slide 21
control signal 0/1
pressure readout
Vacuum system control
arm tunnel, center/end room
BA gauge
ULVAC GI-M2
controller
PLC
Yokogawa
A/D
Yokogawa MW100
Micro IOC
Center control
EPICS
Pirani gauge
Convectron type
Gate valve
（actuator）
Ion pump
VARIAN type
Ion pump
Gamma type
Ethernet
RS485
→ status: 3
← control: 3
→ status: 4
← control: 2
→ status: 2
← control: 1
controller
controller
controller
controller
A gate valves of large diameter takes 40 seconds for closing.
120418 VAC (YS)
KAGRA Vacuum System
3. Final design and quality assurance; (4) Vacuum system operation

## Slide 22
LCGT Vacuum System
120417 VAC (YS)
120418 VAC (YS)
KAGRA Vacuum System
Jul 2014
5) installing chambers in Center Room; Jul 2014
4) carrying tubes and lay on the supports;
        from Apr 2014 to Jun 2014
Jul 2014 to Mar 2015
Jul 2014 to Mar 2015
3) installing chambers in X and Y ends; Apr 2014
Apr 2014
Apr 2014
Apr 2014
22
4. Schedule for installing
1) manufacturing 478 of tubes;
        from Apr 2011 to Mar 2013
2) manufacturing chambers;
        from Sep 2012 to Mar 2014
Finish X-arm at the end of 2014
ETMYA
ITMY
ETMXA
ITMX
BS
PRM
PR3
PR2
SRM
SR3
SR2
PD
MCF
MC
3000 m
IAOX
EAOX
MMT
BRTY
BRTX
IAOY
EAOY
6) jointing tubes and pump down in X and Y arm
        from Jul 2014 to Mar 2015

## Slide 23
** recovery “without breaking arm-vacuum”
  BA gauge failure: grid contamination, filament breakdown
  feedthrough erosion; high voltage feedthrough of ion pump
  power supply/controller erosion; ion pump, turbo molecular pump
  durability for humidity is being examined (50°C-98%, 7 cycle of 8h-operation/98h-off).
** recovery “by re-pumping an arm”
  window (view port) break down
  crack and erosion in bellow joint
  metal gasket erosion
** safety “by closing gate valves (large dia,)”
    electric-power shut down
    anomalous pressure rise
ETMX
ITMX
3000 m
expected pump-down scheme (a 3-km arm)
  to 1 Pa >> few days by dry-pump
  to 10-6 Pa >> 50 hours by TMP
  to 10-7 Pa >> 500 hours by IP
(based on the ougassing rate in test tubes)
IP
TMP
FL P
DRY P
Vacuum component failure and leakage
120418 VAC (YS)
KAGRA Vacuum System
5. Risk management