## Slide 1: My work in 2015 2-1
Hiroki Tanaka

## Slide 2: Measurement of fiber A

## Slide 3: Measurement
We measured Q of monolithic fiber(fiber A).
The peak was 86Hz, 88Hz.
In 86Hz case, the highest Q was 4400, and in 88Hz case, the highest Q was 4100 in room temperature.

## Slide 4: Method to get higher Q 1
I changed the laser, but there was no peak.

## Slide 5: Method to get higher Q 2
We moved the position of
the fiber from the edge of the
circuit of the actuator to the
center of the actuator.
Then, there was a peak in 90.7Hz
(Q=3460)

## Slide 6: Next step
We cooled down the cryostat but there was no peak.
So we are raising the temperature and we will check what’s wrong.