R&D for the gravitational wave detector KAGRA
Yoichi Aso for the KAGRA collaboration
National Astronomical Observatory of Japan
2016/7/13 @ GR21, Columbia University

---
Cryogenic mirrors
Underground
3km
3km
[Speaker Notes: KAGRAは宇宙線研究所がホスト機関となって神岡鉱山の地下に建設中の基線長3kmの干渉計。 坪野研、特に私は検出器本体の設計チームリーダーで、インストール後に装置の調整、改良を行なって目標の感度を出すためのコミッショニング作業の責任者でもある。]

---
Cryogenic Suspension
Mirror Absorption Measurements
300m Filter Cavity
Crystalline Coatings
Cryogenic Thermal Noise Measurements

---
Cryogenic
Suspensions
Room temp.
14m
Cryogenic

---
Cryogenic Payload
(KEK and ICRR)
Cryostat
Type-A
Platform
Marionette &
  Recoil mass
Intermediate mass
& recoil mass
Mirror &
Recoil mass
Prototype Cryo-Payload

---
Bonding techniques
Q ~ 107
Semi-monolithic sapphire
suspension must be realized
to be sufficiently small
thermal noises.
Q ~ 107
Q ~ 108
HCB and Indium bonding on
sapphire satisfies requirements
of mechanical Q.
removable, thin
Practical way to do these
bonding is under testing.
Strong, thin
Installation into KAGRA: 2017 Summer

---
Characterizing mirror absorption
M. Marchio, D. Tatsumi, R. Flaminio
Photo-thermal
Common-path
Interferometry
Sensitivity
1ppm/cm substrate
0.1ppm in coating

---
Current status
System calibration/verification measurements: done
Large sample holder is ready
Measurement of sapphire samples
A small sample
Absorption ranging 30-240ppm
Strong inhomogeneity
Preparing for large samples

---
Coating thermal noise matters
Here

---
Crystalline Coatings
Conventional amorphous coating: high mechanical loss
Low loss coating with high optical performance necessary
G.Cole et al. Nature Photonics 2013

---
2-inch GaAs/AlGaAs transferred to a sapphire substrate
Largest crystalline coating on Sapphire
6ppm scattering
9 large defects
R. Flaminio, Crystalline Mirror Systems, LMA

---
Cryogenic cavities for thermal noise measurement
Mono-crystalline silicon cavities (1550nm)
Cooled down to 5K
Cryogenic operation successful with a large (20cm) cavity
Working on a twin-cavity configuration
Radiation
Shield
Noise estimates @ 20K
Cryocooler
Cavities
seismic
shot noise
thermo-optic
spacer brownian
thermo-elastic
Coating brownian
substrate brownian

---
Squeezing more out of our detectors
There
Here

---
Squeezing: a promising path forward for tackling quantum noises
GEO
M. Evans et al. 2013
Frequency dependent
rotation of squeezing angle
Necessary for full band sensitivity
improvement
E. Oelker et al. 2016

---
TAMA300
300m prototype interferometer
NAOJ Mitaka Campus

---
300m Filter Cavity Experiment
Daisuke Tatsumi, Eleonora Capocasa, Raffaele Flaminio, Matteo Barsuglia, Jérôme Degallaix
Laurent Pinard, Nicolas Straniero, Roman Schnabel, Kentaro Somiya, Yoichi Aso
300m long
10cm diameter mirrors
Finesse ~ 4500
Round trip loss ~ 80ppm

---
Current Status
Suspensions
being installed
Mirrors
Polished

---
Cryogenic Suspension
Mirror Absorption Measurements
300m Filter Cavity
Stay tuned for further developments
Crystalline Coatings
Cryogenic Thermal Noise Measurements